## Slide 1
Motivation
Methodology
Native point defects and impurities in ZnGeN2
Hydrogen-assisted p-type doping
Conclusions
Density functional theory with the Heyd-Scuseria-Ernzerhof[1] functional implemented in VASP[2] [1] J. Heyd, G. Scuseria, M. Ernzerhof, J. Chem. Phys. 124, 219906 (2006) [2] G. Kresse and J. Hafner, Phys. Rev. B 54, 11169 (1996)
Defect formation energies calculated using a 128-atom supercell with electronic corrections.
C. Freysoldt et al., Phys. Status Solidi B 248, 1067 (2011)
Oxygen and hydrogen are donors in ZnGeN2, strong compensation by vacancies (VZn) and antisites (ZnGe)
Fermi level is closest to the CBM (3.19 eV) under Zn-poor conditions.
II-IV-nitrides are a promising class of materials formed from earth-abundant materials that exhibit a wide range of band gaps and spontaneous and piezoelectric polarization moments.
Potential for optoelectronic and electronic devices.
Orthorhombic II-IV-nitride unit cell derived from cation mutation of wurtzite III-nitrides: group III  group II + IV
What are the properties of defects and prospects for controlled doping in these materials?
Acceptor levels due to substitution on Zn, Ge, and N sites
Native point defects in ZnGeN2
lead to insulating material.
AlGe can lead to p-type doping in ZnGeN2.
H-assisted doping increases Al substitution on the Ge site.
PGe is a promising n-type dopant.
This work was supported by the Army Research Office (ARO) under grant number W911NF-16-1-0738. Computational resources were provided by CNSI/MRL, NERSC, and XSEDE.
Variation in Fermi-level pinning due to ON and ZnGe
Defects and Impurities in ZnGeN2
All candidate acceptors have transition levels within the band gap
AlGe has a transition level 0.24 eV from the VBM; similar to Mg in GaN
Quayle, P.C., et al., MRS Comm., 3(3), 135–138. (2013).
Wurtzite GaN
Orthorhombic ZnGeN2
Candidate p-type and n-type dopants in ZnGeN2
Deep versus shallow defects
Defects and Impurities in ZnGeN2
Formation energy of candidate donors
Defects and Doping in ZnGeN2 Nicholas Adamski1, Zhen Zhu2, Darshana Wickramaratne2, Chris G. Van de Walle2 1. Department of Electrical and Computer Engineering, UC Santa Barbara, 2. Materials Department, UC Santa Barbara
Al incorporates on Ge and Zn sites
 strong compensation  limits p-type doping by AlGe
AlGe forms neutral complexes with H similar to MgGa – H in GaN
AlGe – H binding energy calculated to be 0.55 eV
Diffusion barrier for H in ZnGeN2 is 1.2 eV
H can be removed in a post-growth anneal
All candidate donors are shallow
PGe has the lowest formation energy, and least risk of compensation